Supporting information

Towards an ultra-long lifespan Li-CO2: electron structure and charge transfer pathway regulation on hierarchical architecture

Yangyang Wang a, Jing Wang a, Jinming Wang a, Meng Yang a, Guodong Zou a,*, Lanjie Li b, John S. Tse c, Carlos Fernandez d, Qiuming Peng a,*

a State Key Laboratory of Metastable Materials Science and Technology, Yanshan University, Qinhuangdao, 066004, P.R. China

b Chengde Iron and Steel Group Co., Ltd, HBIS Group Co., LTD., Chengde, Hebei 067102, China

c Department of Physics, University of Saskatchewan, Saskatoon, SK, S7N5B2, Canada

d School of Pharmacy and Life Sciences, Robert Gordon University, Aberdeen, AB107GJ, United Kingdom

*Corresponding Authors: zouguodong@ysu.edu.cn, pengqiuming@ysu.edu.cn

Supporting tables.

Table S1. Fitting parameters of EIS curves of the CPM-0.1MnO2， CPM, and CP-0.1MnO2 sample in terms of fitting circuits, respectively.

| Samples | states | Re (Ω) | Rf (Ω) | Q1 |  | Rct | Q2 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Y | n | (Ω) | Y | n |  |
| CPM-0.1MnO2 | Pristine | 24.51 | 18.67 | 3.3×10-2 | 0.8 | 78.5 | 3.3×10-5 | 0.8 |
|  | 1st Discharge | 34.25 | 44.31 | 5.8×10-3 | 0.86 | 261.8 | 1.58×10-5 | 0.69 |
|  | 1st Charge | 36.53 | 23.6 | 3.67×10-5 | 0.68 | 86.81 | 1.7×10-5 | 0.83 |
| CPM | Pristine | 18.57 | 3.67 | 9.4×10-3 | 0.8 | 102.63 | 6.7×10-5 | 0.8 |
|  | 1st Discharge | 41.8 | 200.9 | 1.7×10-2 | 0.8 | 336.1 | 2.5×10-5 | 0.8 |
|  | 1st Charge | 32.38 | 81.88 | 2.17×10-5 | 0.9 | 154.3 | 2.45×10-5 | 0.6 |
| CP- 0.1MnO2 | Pristine | 34.78 | 28.67 | 5.9×10-6 | 0.64 | 200.8 | 1.14×10-5 | 0.75 |
|  | 1st Discharge | 39.5 | 310 | 7.0×10-3 | 0.8 | 559.3 | 9.6×10-6 | 0.8 |
|  | 1st Charge | 37.49 | 106.8 | 3.5×10-3 | 0.83 | 310.1 | 7.5×10-5 | 0.63 |

Table S2. Comparison and summary of recent literature on electrochemical performances of liquid electrolyte-based Li-CO2 batteries with different cathodes.

| Cathodes | Cycle Time (h)/numbers | Overpotential (V) | I (mA/g) | MAM (mg/cm2) | ACD (μA/cm2) | CAC (μAh/cm2) |
| --- | --- | --- | --- | --- | --- | --- |
| 3D NCNT/G[1] | 3600(180) | 1.13 | 100 | 0.35 | 35 | 350 |  |
| RuP2-NPCF[2] | 2000(200) | 1.3 | 200 | 0.2 | 20 | 200 |  |
| CQD/hG[3] | 235(235) | 1.02 | 1000 | 0.1 | 100 | 50 |  |
| Ir/CNF[4] | 1200(120) | 1.3 | 100 | 0.2 | 20 | 100 |  |
| B-NCNT[5] | 720(360) | 1.96 | 1000 | 0.2 | 200 | 200 |  |
| TDG[6] | 600(600) | 1.01 | 1000 | 0.1 | 100 | 50 |  |
| MoS2(Li-air)[7] | 1400(700) | 1.2 | 500 | 0.1 | 50 | 50 |  |
| W2C-CNTS[8] | 750(75) | 0.30 | 200 | 0.3 | 60 | 300 |  |
| This work | 4348(1087) | 0.47 | 500 | 0.4 | 200 | 400 |  |

Notes: I: Mass current density, MAM: Mass of active material, ACD: Corresponding area current density; CAC: Corresponding area current.

Table S3. Possible reaction pathways about nucleation processes of Li2CO3 on M-MnO2 and MnO2 catalytic surfaces.

| Pathname | Reaction pathway |
| --- | --- |
| Path1 | *Li→*LiCO2→*Li2CO2→*Li2CO3 |
| Path2 | *Li→*LiCO2→*LiCO3→*Li2CO3 |
| Path3 | *CO2→*LiCO2→*Li2CO2→*Li2CO3 |
| Path4 | *CO2→*LiCO2→*LiCO3→*Li2CO3 |
| Parh5 | *CO2→*CO3→*LiCO3→*Li2CO3 |

Table S4. The bond length of Li-O in M-MnO2 and MnO2.

|  | M-MnO2 | MnO2 |
| --- | --- | --- |
| Li1-O1 | 1.942 | 2.074 |
| Li1-O2 | 2.173 | 2.066 |
| Li2-O2 | 1.809 | 2.060 |
| Li2-O3 | -- | 2.069 |

Supporting Figures.

Fig. S1. a) SEM image and b) TEM image of the MXene. c) SEM image of cross-section and d) local magnification of the CPM-0.1MnO2. e) SEM image of the front view and f) corresponding elemental distribution of the CPM-0.1MnO2.

Fig. S2. a) XPS survey spectra of the CP-0.1MnO2 and CPM-0.1MnO2. b-c) XPS profiles of Ti 2p and Mn 2p. d) Raman spectra of the CP, MXene, MnO2 and CPM-0.1MnO2, respectively. e) N2 adsorption-desorption isotherms and f) aperture distribution profile of the CP-MnO2 and CPM-0.1MnO2

Fig. S3. SEM image of a, d) CP-0.1MnO2, b, e) CPM-0.05MnO2 and c, f) CPM-0.2MnO2, respectively.

Fig. S4.The conductivity values of the different electrodes.

Fig. S5. a) First discharge-charge curves and b) Polarization gap under a current density of 40 μA cm-2 and a specific capacity of 400 μA h cm-2 with four different cathodes, respectively.

Fig. S6. Voltage profiles of the Li-CO2 battery with CPM-0.1MnO2 cathodes in pure Ar between 2.5 and 4.2 V at 200 μA cm-2.

Fig. S7. a-c) Polarization gap for 400 μA h cm-2 capacity at different current densities and cycle numbers in CPM-0.1MnO2, respectively.

Fig. S8. Discharge/charge profiles, and corresponding time-voltage curves at a-b) 40, and c-d) 80 μA cm-2 in CPM-0.1MnO2, respectively.

Fig. S9. Discharge-charge cycling stability at 40 μA cm-2 for a) CP, b) CPM, c) CP-0.1MnO2 d) CPM-0.05MnO2, e) CPM-0.2MnO2 and f) MXene-0.1MnO2 with a cut-off capacity of 400 μA h cm-2, respectively.

Fig. S10. The rate capabilities of the Li-CO2 batteries with different cathodes.

Fig. S11. Full discharge/charge profiles of CPM, CP-0.1MnO2 and CPM-0.1MnO2 tested at 40 μA cm-2, respectively.

Fig. S12. a-b) Ex-situ XPS profiles of Li 1s, and C1s different states in CPM-0.1MnO2 (a: Pristine, c: Discharge, e: Recharge), respectively. c-d) XPS profiles of Li 1s, and C1s in CPM-0.1MnO2 and CPM-0.1MnO2 after 200cycles, respectively.

Fig. S13. The EIS determined the impedance of the battery under three states of electrodes with a) CPM, b) CP-0.1MnO2 and c) CPM-0.1MnO2, respectively. d) The corresponding fitting circuits.

Fig. S14. SEM images of a-b) CP-0.1MnO2 and c-d) CPM-based cathode in different stages.

Fig. S15. In situ gas evolution profiles of the Li-CO2 batteries with a) CPM-0.1MnO2 and b) CP-0.1MnO2 during charge.

Fig. S16. Top and sight views of optimized energetically favorable structures of a-c) Li and d-f) CO2 adsorbed on MnO2, MXene and M-MnO2 surface, respectively.

Fig. S17. Sight views of optimized energetically favorable structures of Li2CO3 adsorbed on a) M-MnO2 and b) MnO2 surface, respectively. Top and sight views of optimized energetically favorable structures of Li2CO3 adsorbed on c-d) MXene surface.

Fig. S18. Charge changes of Li2CO3 adsorbed on a) M-MnO2 and b) MnO2 surfaces, respectively.

Fig. S19.The adsorption models of reaction intermediates on MXene.

Fig. 20. The adsorption models of reaction intermediates on MnO2 and M-MnO2, respectively.

Fig. S21. Top and sight views of the optimized energetically most favorable structures of a-c) Li and d-f) CO2 adsorbed on MnO2, MXene and M-MnO2 surface, respectively.

Fig. S22. Top and sight views of the optimized energetically most favorable structures of Li2CO3 adsorbed on a-b) MXene surface, respectively.

References

(1) Xiao, Y., Du, F., Hu, C., Ding, Y., Wang, Z. L., Roy, A., & Dai, L. ACS Energy Letters, 2020, 5(3), 916-921.

(2) Guo, Z., Li, J., Qi, H., Sun, X., Li, H., Tamirat, A. G., & Wang, L. Small, 2019, 15(29), 1803246.

(3) Jin, Y., Hu, C., Dai, Q., Xiao, Y., Lin, Y., Connell, J. W. & Dai, L. Advanced Functional Materials, 2018, 28(47), 1804630.

(4) Wang, C., Zhang, Q., Zhang, X., Wang, X. G., Xie, Z., & Zhou, Z. Small, 2018, 14(28), 1800641.

(5) Li, X., Zhou, J., Zhang, J., Li, M., Bi, X., Liu, T. & Wang, B. Advanced Materials, 2019, 31(39), 1903852.

(6) Ye, F., Gong, L., Long, Y., Talapaneni, S. N., Zhang, L., Xiao, Y., & Dai, L. Advanced Energy Materials, 2021, 11(30), 2101390.

(7) Asadi, M., Sayahpour, B., Abbasi, P., Ngo, A. T., Karis, K., Jokisaari, J. R., & Salehi-Khojin, A. Nature, 2018, 555(7697), 502-506.

(8) Zhang, X., Wang, T., Yang, Y., Zhang, X., Lu, Z., Wang, J., & Yao, J. ACS Energy Letters, 2021, 6(10), 3503-3510.