Supporting information

Wave-Layered Dendrite-Free Lithium Deposition with Unprecedented Long-Term Cyclability

Jiawen Feng1, Bingcheng Ge1,2*, Jing Wang1, Lu Zhang1, Di Liu1, Guodong Zou1, John S. Tse3, Carlos Fernandez4, Xiaobing Yan5, Qiuming Peng1*

1State Key Laboratory of Metastable Materials Science and Technology, Yanshan University, Qinhuangdao, 066004, P.R. China

2Department of Mechanical Engineering, Research Institute for Smart Energy, The Hong Kong Polytechnic University, Hong Kong, China

3Department of Physics, University of Saskatchewan, Saskatoon, SK, S7N5B2, Canada

4School of Pharmacy and Life Sciences, Robert Gordon University, Aberdeen, AB107GJ, United Kingdom

5Key Laboratory of Brain-Like Neuromorphic Devices and Systems of Hebei Province, College of Electronic and Information Engineering, Hebei University, Baoding 071002, P.R. China

Corresponding author: pengqiuming@ysu.edu.cn

bingcheng.ge@polyu.edu.hk

Supporting Experimental Sections

Structural characterization

Powder X-ray diffraction (XRD) patterns were collected on an X-ray diffraction (Rigaku D/MAX-2005/PC) using a filtered Cu Kα radiation at a sweep rate of 2 degree/min, XRD refinement was performed using TOPAS v.5.0 software. The micro-morphologies were observed with FEI Helios G4CX with an accelerating voltage of 5 kV for SEM image capture. Transmission electron microscope (TEM), and elemental mapping were observed on a Talos F200X at 200 kV. The specific surface areas and pore size distribution were measured by a Micromeritics ASAP2020 using nitrogen gas adsorption at 77 K (-196 oC). X-ray photoelectron spectroscopy (XPS) patterns were conducted on a ThermoFisher with Al Kα (1486.71 eV) X-ray radiation (15 kV and 10 mA). The binding energies obtained in the XPS analysis were corrected by referencing the C 1s peak position (284.60 eV). Raman spectroscopy was obtained from Renishaw micro-Raman spectroscopy with a laser radiation of 514 nm.

Electrochemical test

The galvanostatic discharge/charge tests were collected on a LAND CT2001A battery test instrument. The specific capacity and current density were calculated according to the area of the electrodes. Electrochemical impedance spectroscopy (EIS) curves were carried out on a BioLogic VMP3 system with the typical frequency range from 100 kHz to 10 mHz by applying the applied voltage of 5 mV.

Supporting Tables

Table S1. The fitting results in terms of EIS curves.

| Samples | Cycle (number) | Re (Ω) | Rf (Ω) | Rct (Ω) |
| --- | --- | --- | --- | --- |
| Li | 1 | 60.0 | 205.40 | 89.12 |
| Li | 10 | 17.3 | 294.20 | 79.48 |
| Li | 20 | 21.9 | 220.60 | 82.95 |
| P-CC/Li | 1 | 85.0 | 197.49 | 56.14 |
| P-CC/Li | 10 | 40.0 | 313.12 | 45.62 |
| P-CC/Li | 20 | 49.5 | 184.63 | 58.55 |
| P-CC/Li3N/Li | 1 | 64.5 | 189.30 | 57.60 |
| P-CC/Li3N/Li | 10 | 8.4 | 275.10 | 52.60 |

Supporting Figures

Figure S1. Adsorption of a single Li atom on different crystal planes of metallic Li.

Figure S2. The arrangement of (a, d) 4, (b, e) 9 and (c, f) 16 Li on the Li(001) crystal plane

Figure S3. The growth of 4 Li atoms on the Li3N (001) surface: (a) in plane and (b) stacking.

Figure S4. The growth of 16 Li atoms on the Li3N (001) surface: (a) in plane and (b) stacking.

Figure S5. Layout of multi-layer Li on the Li3N (111) plane.

Figure S6. Variation of adsorption energy of different Li layers on different surfaces of Li (001) plane (a, b) and Li (110) plane (c, d).

Figure S7. ELF of continuous deposition of 4, 9 and 16Li on the plane of Li.

Figure S8. ELF of continuous deposition of 4, 9, 16Li on the plane of Li3N.

Figure S9. (a) SEM image of the CC, (b) cross-section of the original CC, (c) high amplification SEM image of the carbon cloth after joule heat treatment and (d) cross-section of the carbon cloth after joule heat treatment.

Figure S10. (a) N2 adsorption/desorption isotherm curves of CC, (b) P-CCand pore size distribution curves.

Figure S11. (a) Raman spectra of CC and P-CC. High resolution XPS spectra, (b) C 1s of CC sample and (c) C 1s of P-CC sample

Figure S12. Optical images of impregnated molten Li: (a) CC, (b) P-CC/Li and (c) P-CC/Li3N/Li.

Figure S13. SEM images of anode: (a) P-CC/Li and (b) P-CC/Li3N/Li.

Figure S14. The Rietveld analysis on the XRD data of P-CC/Li3N/Li

Figure S15. (a) Li3N particle size distribution diagram (35 particles were counted). (b) Distribution map of area occupied by Li3N (15 SEM images were counted).

Figure S16. The cross-sectional images of P-CC/Li3N/Li(a-c) and pure Li anode(d-f): (a, c) pristine; (b, e) after stripping 10 mAh cm-2; (c, f) after plating 10 mAh cm-2.

Figure S17. SEM images of plating/stripping of P-CC/Li anode at current density of 1 mA cm-2 with a limited capacity of 10 mAh cm-2: (a) original morphology, (b) stripping with lithium of 10 mAh cm-2, and then plating with (c) 5 mAh cm-2 and (d) 10 mAh cm-2, respectively

Figure S18. Deposition morphology of pure Li after 10 cycles (a) and 100 cycles (b), P-CC/Li3N/Li anode after 10 cycles (c) and 100 cycles (d).

Figure S19. EIS of different samples with different cycles: (a) Li, (b) P-CC/Li and (c) P-CC/Li3N/Li, inset: corresponds to the fitting circuit. (1 mAh cm-2 and 1 mA cm-2).

Figure S20. Voltage time of cyclic plating/stripping of lithium at different current densities of the pure Li, P-CC/Li, P-CC/Li3N/Li composite electrodes: (a) 5 mA cm-2, (b) 10 mA cm-2. (c) Rate performance of different samples at different current densities with a stripping/plating capacity of 1 mAh cm-2. (d) Cycle stability of different electrode materials at 10 mAh cm-2 capacity.

Figure S21. Galvanostatic cycling of different symmetric cells at a current density of 10 mA cm-2 with a stripping/plating capacity of 1 mAh cm-2 at (a) -10 °C and (b) 50 °C.

Figure S22. Voltage profile of stripping Li from the P-CC/Li，P-CC/Li3N/Li electrodes to 1 V versus Li+/Li under the current density of 1 mA cm-2.

Figure S23. Typical SEM images of charge and discharge process for the P-CC (a-b) and the original CC (c-d), the discharge (a,c), the state of charge (b,d).

Figure S24. Characterization of the discharge products in the P-CC: (a) XRD patterns corresponding to different states of the sample and (b) XPS spectra corresponding to different states.

Figure S25. Cut-off voltage of discharge terminal at 0.1 mA cm-2 with different electrode materials at limited capacity of 0.5 mAh cm-2.

Figure S26. SEM characterize of the anode after cycles: (a) pure Li, (b) P-CC/Li3N/Li.