## Slide 1: Introduction to Hydrogen & Hydrogen Economy: Opportunities and Challenges
Mamdud Hossain, Nadimul Faisal, Anil Prathuru, Victoria Kurushina, Vinooth Rajendran
School of Engineering, Robert Gordon University, Aberdeen, Scotland
Qiong Cai, Bahman Horri, Ajith Kumar
School of Chemical and Process Engineering, University of Surrey, UK

## Slide 2: Robert Gordon University provides industry led undergraduate and postgraduate courses leading to highly relevant awards and degrees
Student number: 16000 UG 10000, PG 6000
1st in Scotland and 2nd in the UK in the Graduate Employment Rate measure (QS Graduate Employability Rankings 2022)

## Slide 3: Hydrogen is a versatile energy career and is key to decarbonize a number of difficult sectors

## Slide 4: Hydrogen can used in a number of ways to achieve energy transition
Electricity generation: distributed, remote, stand alone, backup (using fuel cell)
Transports: car, bus, truck, forklift, train, ship (using fuel cell)
Chargers: mobile, laptop (using fuel cell)
Domestic heating and electricity (using fuel cell)
Domestic heating and cooking (blended with methane, combustion)
Truck / digger: (blended with diesel)
Energy storage and load balance for intermittent renewable energy: (production, storage and use)

## Slide 5: What is H2?
H2 is a gas. It is colorless, odourless, tasteless, non-toxic and highly combustible
Its density – 0.08375 kg/m3 (comparison: air 1.18 kg/m3)
The most abundant chemical element – contribute 75% of the mass of the universe
But here is the problem – it is very scare as a gas, vast numbers of hydrogen atoms are contained in water, natural gas, plants etc.

## Slide 6: Hydrogen is not available as a gas in nature
It has to be produced from different sources:
Natural gas
Water splitting
Biomass

## Slide 7: Hydrogen and colour coding
Grey H2
Produced by fossil fuels (natural gas, coal)
Emits CO2 in the process
Blue H2
Produced by fossil fuels in combination with CCS
Reduces CO2 emissions in the process
Turquoise H2
Produced by pyrolysis of fossil fuels
Solid carbon as by-product
Produced from water splitting in an electrolyser using electricity generated from renewable sources
Green H2
Purple H2
Produced from water splitting in an electrolyser using electricity from nuclear power plants
Yellow H2
Produced from water splitting in an electrolyser using grid electricity

## Slide 8: Green Hydrogen Production : water + renewable electricity and electrolyser

## Slide 9
Robert Gordon University
Researchers
Dr Victoria Kurushina, PDRF
Vinooth Rajendran, RA
Investigators
Prof Nadimul Faisal
Prof Mamdud Hossain
Dr Anil Prathuru
University of Surrey
Researcher
Dr Ajith Soman, PDRF
Investigators
Dr Bahman Horri
Dr Qiong Cai
EP/W033178/1
Scalable metamaterial thermally sprayed catalyst coatings for nuclear reactor high temperature solid oxide steam electrolysis (METASIS)

## Slide 10: Green H2 cost is high across the whole value chain
Green H2 prices needed to be reduced to 1 $/kg from 4 $ /kg (below the production cost of grey H2)

## Slide 11: Several challenges hampering green hydrogen taking bigger role
Technical challenges
  Green hydrogen production from water electrolysis: 60-70% (1/3rd of electricity wasted in heat)
  Hydrogen compression and storage: 10% loss
  Electricity production in fuel cell: 40-55%
  Electricity to Hydrogen to Electricity: 38%
  Work with excess Renewable Energy to improve efficiency.

## Slide 12: Only 1% of world water is fresh water
1 kg H2 production needs more than 20 kg of water (stochiometric, 1 kg H2 uses 9 kg water)
Seawater desalination using reverse osmosis is expensive: (50% efficient and 1 m3 water costs 0.7-2.5 $).

## Slide 13: Electricity accounts for 50-70% of the production cost of Hydrogen
Renewables are intermittent and thus it is difficult to optimise green hydrogen production systems
The price of fuel cells and electrolysers depends on the use of Nobel materials such as platinum.
Platinum is scare material, considerably high cost and resource is concentrated and short supply.
Geopolitical problem due to the location of mines in social or politically unstable locations.

## Slide 14: Electrolyser materials are expensive rare and degrades quickly

## Slide 15: Solid Oxide Electrolyser Working Principle
Cathode: H2O + 2e- = H2 +O2-
Anode: O2- = ½ O2 + 2e-
Overall: H2O = H2 + ½ O2
Cathode: Ni-YSZ porous, 500 µm
Electrolyte: YSZ dense, ion conductor, 20 µm
Anode: LSM-YSZ, 50 µm
Length: 0.4m

## Slide 16: SOEL Cell designs
+ Good cell stability during electrochemical process
- High resistance for polarization
+ High mechanical robustness
+ Good gas diffusion properties
- High ohmic losses in the thickened electrolyte layer
+ Lower operating temperature
+ Low ohmic resistance
+ Lower costs of material
+ Considered to be easier for fabrication
- Lower mechanical reliability
+ High mechanical stability
- Energy losses in the supporting porous metal layer
Thick metal
Thick anode
Thick electrolyte
Thick cathode
Support type
Electrolyte-supported cell
Anode-supported cell
Cathode-supported cell
Metal-supported cell

## Slide 17
Porous cathode layer (NiO-GDC) (40-50 μm thick); 30-40% porosity – Dip coating
Dense electrolyte layer (GDC) (10-20 μm thick); 0% porosity – Dip coating
Porous substrate (SS or Ti) (2.15 mm thick, 100 mm long); 50-70% porosity
Metasurface (1 mm x 1 mm x 50 μm); 50-70% porosity
Current collector (silver mesh or silver wire wrapped)
Interconnect layer (silver + NiO thin film: ~10 microns)
Porous cathode functional layer (NiO-GDC) (10-20 μm thick); 20-30% porosity – Dip coating
Dense electrolyte double layer (YSZ) (1-2 μm thick); 0% porosity – Dip coating
Porous anode functional layer (GDC-LSCF) (10-20 μm thick); 20-30% porosity – Dip coating
Porous anode layer (GDC-LSCF) (40-50 μm thick); 30-40% porosity - Dip coating
Current collector (silver mesh or silver wire wrapped)
230 microns
2.15 mm
Air flow
Steam in
Steam out
Interconnect layer (silver + GDC thin film: ~10 microns); 30-40% porosity
Plan A – Dip coating

## Slide 18
Porous cathode layer (NiO-YSZ) (40-50 μm thick); 30-40% porosity – Thermal spray
Dense electrolyte layer (YSZ) (10-20 μm thick); 0% porosity – Dip coating
Porous substrate (SS or Ti) (2.15 mm thick, 100 mm long); 50-70% porosity
Metasurface (1 mm x 1 mm x 50 μm); 50-70% porosity
Current collector (silver mesh or silver wire wrapped)
Interconnect layer (silver + NiO thin film: ~10 microns)
Porous cathode functional layer (NiO-YSZ) (10-20 μm thick); 20-30% porosity – Dip coating
Dense electrolyte double layer (YSZ) (1-2 μm thick); 0% porosity – Dip coating
Porous anode functional layer (YSZ-LSCF) (10-20 μm thick); 20-30% porosity– Dip coating
Porous anode layer (YSZ-LSM) (40-50 μm thick); 30-40% porosity - Thermal spray
Current collector (silver mesh or silver wire wrapped)
230 microns
2.15 mm
Air flow
Steam in
Steam out
Interconnect layer (silver + GDC thin film: ~10 microns); 30-40% porosity
Plan B - Dip coating and thermal spray

## Slide 19
Back Scattered Electron image & Elemental mapping of SS/Ag/NiO-YSZ coating
Cross sectional morphology of tubular SS supported NiO-YSZ (60:40 wt%) cathode layer
Combinations | Area %
Steel | 36.48
Mounting Resin | 43.08
ZrO2 | 1.53
2NiO | 11.42
Ag | 0.60
Ni rich | 6.89
94 µm
350 µm

## Slide 20: Experimental Tests
Our targets
Improving efficiency
Lower cost
Durability
Scalability & system integration
High temperature tests to be performed in the University of Surrey
Material characterization tests to be performed in the Robert Gordon University
20

## Slide 21: Electrochemistry
]

## Slide 22: CFD modelling
Continuity and momentum
Heat transfer
Species concertation (i.e. H2O, H2, O2)
Species source term:

## Slide 23: CFD modelling
Electron and ionic transport:
Gas phase diffusivity through porous electrodes – multicomponent diffusivity, or dilute gas and Knudsen diffusivity

## Slide 24: An I-V curve is an effective way to explain SOEL performance
Higher current density, higher production rate of H2, but higher voltage i.e. higher power required
Main losses: Anode activation loss, then cathode activation loss and ohmic loss
Operating at 1023 K
J. Udagawa et al. (2007) -doi:10.1016/j.jpowsour.2008.01.069

## Slide 25: An I-V curve is an effective way to explain SOEL performance
Higher temperature leads to better performance due to reduction in anode and cathode activation overpotential. However, it creates thermal stress and less durable cells
J. Udagawa et al. (2007) -doi:10.1016/j.jpowsour.2008.01.069

## Slide 26: CFD Modelling
Plane Cell
Metasurface cell

## Slide 27: Comparison with previous studies

## Slide 28: Different Meta Surfaces

## Slide 29: Mestasurface meshes

## Slide 30: CFD Simulation – comparision of metasurfaces

## Slide 31: Optimisation of met surface geometry

## Slide 33: Summary
Metasurface elements applied for solid oxide electrolysers open a new design space of potential cell improvements.
the best performance curve belongs to the net structure, among the studied options, with up to 8.58% improvement compared to the case without the metasurface
Acknowledgements
The authors acknowledge high temperature steam electrolysis related funding by the UKRI EPSRC via Grant No. EP/W033178/1 (METASIS).

## Slide 34
Robert Gordon University
Any Question?